| [1] | Draft Heat treatment of wood using dielectric heating (2007-114) |
| --- | --- |
| [2] | Status box This is not an official part of the standard and it will be modified by the IPPC Secretariat after adoption. Date of this document 2015-01-22 Document category Draft Annex to ISPM 28 Current document stage To 2015-07 member consultation Major stages 2006-04 CPM-1 (2006) added topic Revision of ISPM 15 (Regulation of wood packaging material in international trade) (2006-011) 2006-12 Treatment submitted in response to 2006-08 call for treatments 2007-07 Revised text considered by TPFQ 2007-12 Further revised text submitted to TPPT 2009-07 Amended text considered by TPFQ 2009-10 Additional information submitted to TPPT 2010-07 Text updated 2010-11 SC added topic Microwave irradiation of wood packaging material (2007-114) 2011-03 Text submitted to SC e-discussion forum and revised based on SC comments; text submitted to SC e-discussion poll 2011-05 SC approved for member consultation 2011-07 member consultation 2011-10 TPPT Response to comments to SC 2013-07 TPPT at its meeting changed the title to Heat treatment of wood using dielectric heating and deferred treatment review pending publication of important research then underway 2014-06 TPPT recommended draft treatment to SC for MC 2014-08 Draft treatment submitted to SC e-discussion forum; SC returned draft treatment to TPPT with comments 2014-09 TPPT revised draft treatment in response to SC comments 2014-10 SC approved for member consultation via online poll Treatment Lead Mr Mike ORMSBY (NZ) Secretariat notes 2011-05 Formatted and revised according to changes made to draft annex 1 to ISPM 15 2013-12 Secretariat updated the List of topics for IPPC standards before CPM-9 (2014) based on TPPT decision to change the title 2015-01 Edited |
| [3] | Scope of the treatment |
| [4] | This treatment comprises the dielectric1 heating of wood to reduce the likelihood of introduction and spread of Bursaphelenchus xylophilus and those pest insects and fungi likely to be associated with wood in international trade2. |
| [5] | Treatment description |
| [6] | Name of treatment Heat treatment of wood using dielectric heating |
| [7] | Active ingredient N/A |
| [8] | Treatment type Physical (heat) |
| [9] | Target pests Wood-borne life stages of insects, fungi and Bursaphelenchus xylophilus (Steiner & Buhrer) Nickle (Nematoda: Aphelenchoididae) |
| [10] | Target regulated articles Wood |
| [11] | Treatment schedule |
| [12] | Where the application of heat is undertaken using dielectric heating (e.g. microwaves or radio waves), wood must be heated to achieve a minimum temperature of 60 ˚C for the duration of 1 minute throughout the profile of the wood. |
| [13] | This treatment schedule achieves no less than a 99.99683% level of mortality for all life stages of B. xylophilus at the 95% confidence level, and it is effective against those pest insects and fungi likely to be associated with wood in international trade. |
| [14] | Other relevant information |
| [15] | The Technical Panel on Phytosanitary Treatments based its evaluation of this treatment for B. xylophilus on the research reported by Hoover et al. (2010) and Janowiak et al. (2014). As insects have been found to be generally more susceptible to heat than pine wood nematodes are, the level of efficacy for insects will be equivalent to or higher than that for nematodes. |
| [16] | The effectiveness of this treatment against other pest insects and fungi has been supported by Fleming et al. (2003, 2004), Henin et al. (2008), NAPPO (2013), Soma et al. (2002, 2003), Tomminen and Nuorteva (1992) and Tomminen et al. (1991). |
| [17] | Because some sources of dielectric heating will result in limited initial heat penetration, further time may be required to allow heat diffusion through the wood after exposure to dielectric heating in order to achieve the treatment schedule throughout the profile of the wood. |
| [18] | References |
| [19] | Fleming, M., Hoover, K., Janowiak, J., Fang, Y., Wang, X., Liu, W., Wang, Y., Hang, X., Agrawal, D., Mastro, V. & Roy, R. 2003. Microwave irradiation of solid wood packing material (pallet and crate lumber): An effective technique to destroy the Asian longhorned beetle (Anoplophora glabripennis) hitchhiking to the United States. Forest Products Journal, 52: 1–7. |
| [20] | Fleming, M.R., Janowiak, J.J., Kearns, J., Shield, J.E., Roy, R., Agrawal, D.K., Bauer, L.S., Miller, D.L. & Hoover, K. 2004. Parameters for scale-up of microwave treatment to eradicate cerambycid larvae infesting solid wood packing materials. Forest Products Journal, 54(7/8): 80–84. |
| [21] | Henin, J.-M., Charron, S., Luypaert, P.J., Jourez, B. & Hebert, J. 2008. Strategy to control the effectiveness of microwave treatment of wood in the framework of the implementation of ISPM 15. Forest Products Journal, 58: 75–81. |
| [22] | Hoover, K., Uzunovic, A., Gething, B., Dale, A., Leung, K., Ostiguy, N. & Janowiak, J.J. 2010. Lethal temperature for pinewood nematode, Bursaphelenchus xylophilus, in infested wood using microwave energy. Journal of Nematology, 42: 101–110. |
| [23] | Janowiak, J., Dubey, M., Hoover, K., Mack, R., Elder, P. 2014. Comparative study of radio frequency (RF) and microwave (MW) heating of wood in compliance with ISPM 15 phytosanitary treatment. Presentation to the 2014 meeting of the International Forest Quarantine Research Group. Rome, 2014. 35 pp. |
| [24] | NAPPO (North American Plant Protection Organization). 2013. Review of heat treatment of wood and wood packaging. ST 03. Ottawa, NAPPO Forestry Panel. |
| [25] | Soma, Y., Goto, M., Naito, H., Ogawa, N., Kawakami, F., Hirata, K., Komatsu, H. & Matsumoto, Y. 2003. Effects of some fumigants on mortality of pine wood nematode, Bursaphelenchus xylophilus infecting wooden packages. 3. Mortality and fumigation standards for pine wood nematode by methyl bromide. Research Bulletin of the Plant Protection Service Japan, 39: 7–14. |
| [26] | Soma, Y., Naito, H., Misumi, T., Tsuchiya, Y., Mizobuchi, M., Matsuoka, I., Kawakami, F., Hirata, K. & Komatsu, H. 2002. Effects of some fumigants on pine wood nematode, Bursaphelenchus xylophilus infecting wooden packages. 2. Mortality of pine wood nematode by methyl bromide tent fumigation. Research Bulletin of the Plant Protection Service Japan, 38: 13–19. |
| [27] | Tomminen, J., Halik, S. & Bergdahl, D.R. 1991. Incubation temperature and time effects on life stages of Bursaphelenchus xylophilus in wood chips. Journal of Nematology, 23: 477–484. |
| [28] | Tomminen, J. & Nuorteva, M. 1992. Pinewood nematode, Bursaphelenchus xylophilus in commercial sawn wood and its control by kiln-heating. Scandinavian Journal of Forest Research, 7: 113–120. |
| [29] | Footnote 1: Dielectric heating is based on the alternating electrical field of the electromagnetic wave emitted by the dielectric radiation source (e.g. microwave or radio wave). Chemical compounds with asymmetric charge distribution, so called dipole characters (e.g. water), tend to orientate along this electrical field and oscillate with the electrical field (e.g. 2.45 MHz causes 2.45 million oscillations per second). The friction generated through this process converts electrical energy into heat energy. |
| [30] | Footnote 2: The scope of phytosanitary treatments does not include issues related to pesticide registration or other domestic requirements for approval of treatments. Treatments also do not provide information on specific effects on human health or food safety, which should be addressed using domestic procedures prior to approval of a treatment. In addition, potential effects of treatments on product quality are considered for some host commodities before their international adoption. However, evaluation of any effects of a treatment on the quality of commodities may require additional consideration. There is no obligation for a contracting party to approve, register or adopt the treatments for use in its territory. |